## Slide 1: Flattening of plates
Tecnologia de Estaleiros Navais
2012

## Slide 2: Preparation of surface

## Slide 3: Flattening - Storage
Plate’s Roller

## Slide 4: Plate’s Roller
Alternate bending

## Slide 5: Flattening – hammer & press
Creation of deformation
Circular action decreasing from the centre
No action near the edges

## Slide 6: Removal a deformation with hammer
Circular action
  Avoid to hit the contour of the plate
  Not applicable when having multiple deformations

## Slide 7: Removing a deformation with hammer
Radial action
Parallel action

## Slide 8: Removing a deformation with hammer
Multiple defects
Stretching
  Hammer concave surface

## Slide 9: Plate’s flattening by heat
Half thickness heating
Points of heating

## Slide 10: Mechanical flattening
Press
  http://www.tyhi.com.cn/press/40mnypj.html

## Slide 11: Tolerances
Localização | Location | Tolerance (mm)
Convés e duplo-fundo | Deck and double-bottom | 8
Pavimentos Cobertos Expostos | Superstructure Covered Not covered | 12 8
Cobertas | Intermediate decks | 10
Superestrutura Anteparas externas Anteparas internas Revestidas Não revestidas | Superstructure External Internal Covered Not covered | 10 12 8
Anteparas estruturais | Bulkheads | 10
Longarinas e sicórdias | Structural Girders | 8

## Slide 12: Measurements at inspection

## Slide 13: Flattening by line heating

## Slide 15: Flattening of panels

## Slide 16: Flattening of panels

## Slide 17: Correction to welding distortions
Oblique heating
  Angle: 30º
  Length: 200 mm
  Width is function of the thickness

## Slide 18: Multi-flame method

## Slide 20: 1st phase

## Slide 21: Second phase

## Slide 22: Corrections to superstructures